Mild Steel bar trial on Drawbench 9/9/24

We started with 2 bars .985 diameter and cut into 4~5-foot lengths.

One bar of the material was found to be Alloy 601, use 2 bars 20’ of Westfield Steel.

The material started out to be .985 and the plan was to swage down to .770. This swaged point would get us through the first two draws. The first draw was done with a .909 draw die with a 1.045 pressure die. This calculates into a 14.8% reduction.

We were targeting around 15% reduction on each pass, but it depended on what dies we had available.

The entire soap box assembly was taken apart and each item was cleaned and put back together.

A laser was used to line up the gripper to the die holder block.

The bars were pointed on the Fenn. We did not  have a .770 die, so we had to use the .764. This reduction from .985 to .764 would allow us to complete the first two pulls before the need to swage down again.

FIRST PULL   .985

Forming die = .909

Pressure die = 1.045

1st Bar

The bar was a little crooked on the swaged end to start with. When it was being pulled, it came out a little crooked on the end with the swage. We tried to adjust it to see if the bent.

2nd Bar

We bent this bar on purpose into a 90-degree bend to see if the drawbench would straighten the bar. The bar was straightened, but the die had severe galling  and had material left inside the die. This was the .909 die. We had to change dies to .913.

3rd Bar

When we were using the .913 die, the bar ran through fine, but the bar was bent upwards a little. We set up the laser again and adjusted the die block down.

4th Bar

Made adjustment again to the die face with laser. We made a very small change to tilt the top of the die face down to see if we could get the downward bend corrected. Ran the chain very slow at start until the carriage hook lifted up then turned the chain speed up to 10. The bar  had a slight bend downward but we will see how it does on the 2nd reduction

2nd PULL   .905

Forming die = .835

Pressure die = .976

1st Bar

The bar still had a slight bend downward. Made an adjustment with laser to compensate for the downward bend. Bars are straighter.

2nd Bar

The bar still has a downward bend. We are placing the bar in the die block with the bend upward and see if it will correct on the second draw. The bar came out a little straighter, but there was still a slight bend.

3rd Bar

Moved the top of the die block forward and the bottom back by using the laser. The bar came out straight, but still not dead-on center. Bars are much straighter than before.

4th Bar

Placed the bar in and it started to bend to the side rather than downward. Used the laser to see if we could find out why. No changes we made would have caused it to go to the side.

3rd PULL   .835

Forming die = .713  .770

Pressure die = .819

.

1St Bar

The bar was placed in the die and it got stuck in the die. The bar broke down close to the gripper. The wrong math was used in the reduction and it was too aggressive. The die was removed, and we place in a .770 die rather than.713.

2nd Bar

The bar pulled good with a slight right bend. Used the laser to adjust for the next pull.

3rd Bar

The bar pulled smoothly. There was a slight down and left bend made on the front of the bar.

4th Bar

The bar pulled smoothly and was straight. This bar should be acceptable to run in the grinders.

We have concluded, the adjustment on the die block is very difficult to dial in by using the 4 bolts to tighten and loosen each one to get the correct alignment. There are variables with the die rings and the die sizes. We have some 3 inch, 4 inch and 5 inch dies which require different die rings to hold them in place. Whenever we have to remove the dies to clean them out, which is every 3 pulls, the angles change slightly. We are going to make soap boxes which will be used for each of the sizes of dies.